DENSITY FUNCTIONAL THEORY EVALUATION OF VANADIC ACID ZEOLITE Y DEALUMINATION IN RESIDUE FLUID CATALYTIC CRACKING REGENERATOR

BY

Ahmad Usman Shehu

U19CE1068

A RESEARCH PROJECT SUBMITTED TO THE DEPARTMENT OF CHEMICAL ENGINEERING,

FACULTY OF ENGINEERING, AHMADU BELLO UNIVERSITY, ZARIA,

IN PARTIAL FULFILMENT OF THE REQUIREMENTS FOR THE AWARD OF THE DEGREE OF

BACHELOR OF ENGINEERING (B.ENG.) IN CHEMICAL ENGINEERING

NOVEMBER, 2026

# DECLARATION

I declare that this project, entitled “Density Functional Theory Evaluation of Vanadic Acid Zeolite Y Dealumination in Residue Fluid Catalytic Cracking Regenerator,” was carried out by me in the Department of Chemical Engineering, Ahmadu Bello University, Zaria. Sources used in the work have been acknowledged in the text and listed in the references. This project has not been submitted, in whole or in part, for another degree or diploma at this or any other institution.

_______________________________ Ahmad Usman Shehu (Student)

_______________________________ Date

# CERTIFICATION

This project, entitled “Density Functional Theory Evaluation of Vanadic Acid Zeolite Y Dealumination in Residue Fluid Catalytic Cracking Regenerator,” was carried out by Ahmad Usman Shehu (U19CE1068). It is submitted to the Department of Chemical Engineering, Ahmadu Bello University, Zaria, in partial fulfilment of the requirements for the award of the degree of Bachelor of Engineering in Chemical Engineering.

_______________________________ Project Supervisor                         Date

_______________________________ Head of Department                         Date

_______________________________ External Examiner                          Date

# DEDICATION

This work is dedicated to my parents for their support throughout my education.

# ACKNOWLEDGEMENTS

I thank my project supervisor for guidance and for the detailed comments that improved this work. I also thank the Head of Department and the academic and technical staff of the Department of Chemical Engineering, Ahmadu Bello University, Zaria, for their support during my studies.

I am grateful to my family and colleagues for their encouragement. I acknowledge the researchers whose published work informed this project and provided the scientific background for the study.

# ABSTRACT

Vanadium contamination reduced Zeolite Y activity in residue fluid catalytic cracking (RFCC). Proposed mechanisms attributed framework damage to vanadic acid or steam hydrolysis. This study compared vanadic acid (H3VO4) and water at a model Zeolite Y Brønsted acid site using a 22-atom AlSi4O4H13 cluster. Initial geometries were screened with GFN2-xTB, optimised with B3LYP-D3(BJ)/def2-TZVP, and checked with PBE0 single-point calculations. Harmonic Gibbs energies were calculated at 298.15 and 1003.15 K. B3LYP and PBE0 favoured vanadic acid electronically by 14.69 and 14.44 kJ mol-1, respectively, while harmonic Gibbs energies favoured water by 11.82 and 66.36 kJ mol-1 at the two temperatures. Vanadic acid formed Al···O and V···O contacts of 1.947 and 2.274 Å; water formed two hydrogen bonds with H···O distances of 1.587 and 1.825 Å. A formal competitive-site estimate using regenerator partial pressures gave a water-to-vanadic-acid site-fraction ratio of 5.7 × 107 to 5.7 × 108. The GFN2-xTB search yielded a 160.70 kJ mol-1 candidate barrier for the first Al–O cleavage step; Appendix A records the DFT frequency and water-path displacement assessments. Electronic binding and high-temperature site occupation favoured different adsorbates. Larger pore-aware models and validated DFT reaction paths were recommended.

TABLE OF CONTENTS

LIST OF TABLES

Table 2.1: Proposed explanations for vanadium-related damage to Zeolite Y

Table 4.1: Accepted DFT reference and adsorption minima

Table 4.2: Selected aluminium–oxygen distances in converged DFT structures (Å)

Table 4.3: Electronic adsorption energies of vanadic acid and water (kJ mol-1)

Table 4.4: Relative electronic energies of converged post-adsorption minima (kJ mol-1)

Table 4.5: Tier 1 pathway candidates for framework Al–O cleavage and water hydrolysis

Table 4.6: Harmonic standard Gibbs energies of adsorption relative to the separated cluster and adsorbate (kJ mol-1)

Table 4.7: Formal single-site occupation estimate at 1003.15 K

Table A.1: DFT reference, adsorption, and pathway calculation register

Table A.2: PBE0 counterpoise ghost-fragment calculation register

Table A.3: Tier 1 pathway candidate and two-sided displacement register

Table B.1: Electronic and harmonic Gibbs-energy terms for accepted DFT states (kJ mol-1)

LIST OF FIGURES

Figure 2.1: Structure of Zeolite Y showing the supercage and its twelve-membered-ring opening

Figure 2.2: Calculated reaction paths for dealumination and desilication using gas-phase and adsorbed water references

Figure 2.3: Transmission electron micrographs of ultra-stable Y zeolite before and after vanadium contamination and steaming

Figure 3.1: Structure-screening, DFT, pathway, and thermochemistry workflow

Figure 3.2: Zeolite Y cluster AlSi4O4H13, vanadic acid, and water used in the calculations

Figure 4.1: Optimised adsorption complexes at B3LYP-D3(BJ)/def2-TZVP. Left, vanadic acid (V-PRC); right, water (W-PRC)

CHAPTER ONE

# 1.0 INTRODUCTION

## 1.1 Background of the Study

In residue fluid catalytic cracking (RFCC), the catalyst repeatedly moves between a reactor and a hot regenerator. Each cycle exposes Zeolite Y to heavy-feed contaminants and steam, placing its aluminium-bearing framework and acid sites under stress. Vanadium accumulates on the catalyst and is linked to a loss of cracking activity, but the molecular route from metal deposition to framework damage remains uncertain.

Steam hydrolyses framework Al–O–Si bonds during regeneration and removes framework aluminium. Each framework aluminium atom is associated with a Brønsted acid site; dealumination therefore reduces the number of sites available for cracking (Malola, Svelle, Lønstad Bleken, & Swang, 2012). This loss of acid sites links framework damage to catalyst activity.

Three explanations describe vanadium-related damage. Wormsbecher et al. (1986) proposed that vanadium oxide reacts with steam to form volatile vanadic acid, which attacks the zeolite. Pine (1990) attributed the main framework attack to steam and assigned vanadium a catalytic or secondary role. Xu, Liu, and Madon (2002) proposed a sodium-mediated route in which vanadium mobilises sodium and steam enables sodium hydroxide attack. These explanations focus on vanadic acid, steam, and sodium, respectively.

Wormsbecher et al. (1986) estimated low-parts-per-million vanadic-acid levels for a high-steam regenerator at about 2 atm. Water therefore occupies a much larger fraction of the bulk gas under those conditions. Comparing both adsorbates at the same model acid site clarifies their electronic and thermochemical preferences within this environment.

## 1.2 Statement of the Problem

Vanadium contamination is associated with accelerated loss of Zeolite Y activity, while the molecular explanation remains debated. The proposed mechanisms assign different roles to vanadic acid, steam, and sodium (Pine, 1990; Trujillo et al., 1997; Xu et al., 2002; Wormsbecher et al., 1986). A common-site comparison of vanadic acid and water provides a focused way to evaluate their relative adsorption and thermochemical preferences.

The present work examined these adsorbates at one Zeolite Y Brønsted acid site and assessed candidate pathways for framework Al–O cleavage. The resulting adsorption energies, pathway assessment, and high-temperature site-occupation estimate provide molecular-level evidence for interpreting the mechanisms reviewed in Chapter Two. These measures separate molecular association from the chemical steps involved in framework damage.

## 1.3 Aim and Objectives of the Study

The aim was to compare vanadic acid and water at a model Zeolite Y Brønsted acid site and assess their implications for dealumination.

The objectives were to:

1. construct and optimise a local Zeolite Y cluster and the initial vanadic-acid and water adsorption structures using ORCA;

2. calculate and compare the electronic adsorption energies of the selected vanadic-acid and water structures;

3. assess candidate pathways for the first framework Al–O cleavage step in the vanadic-acid route and a water-hydrolysis control; and

4. calculate harmonic Gibbs energies at 298.15 K and 1003.15 K and evaluate conditional competitive site occupation using RFCC gas partial pressures from the literature.

## 1.4 Scope and Limitations

The calculations used a gas-phase AlSi4O4H13 cluster representing one Zeolite Y Brønsted acid site. Vanadic acid (H3VO4) and water (H2O) were compared at this site. GFN2-xTB screened initial structures and pathway candidates; selected structures were optimised at B3LYP-D3(BJ)/def2-TZVP, and PBE0-D3(BJ)/def2-TZVP single-point energies checked the electronic comparison. Harmonic Gibbs energies were evaluated at 298.15 K and 1003.15 K, and the high-temperature values were combined with literature gas partial pressures in a single-site equilibrium estimate.

The model describes a local acid-site environment, with terminal hydrogen atoms fixed at the cluster boundary. Its thermochemical estimates use ideal-gas standard states, one equivalent adsorption site, and independent adsorbates. Pore confinement, local vanadium enrichment, and exchangeable sodium define extensions for future models. Appendix A provides the calculation register, and Appendix B gives the numerical substitutions behind the reported energies and site fractions.

## 1.5 Justification of the Study

A matched comparison at one model acid site separates electronic binding from harmonic thermochemical preference. This distinction helps interpret the proposed direct vanadic-acid interaction alongside the high steam abundance of an RFCC regenerator. The pathway assessment and conditional site-occupation estimate also identify the molecular quantities most relevant to larger-pore models and experimental comparison (Adanenche et al., 2023; Etim et al., 2018).

CHAPTER TWO

# 2.0 LITERATURE REVIEW

## 2.1 Zeolite Y in Residue Fluid Catalytic Cracking

Residue fluid catalytic cracking processes heavy refinery feeds that contain metals and other contaminants. The catalyst circulates between a reactor and a regenerator, where coke is burned in air and steam. Zeolite Y supplies many of the catalyst's cracking sites, and vanadium carried in the feed can accumulate on the catalyst during operation (Adanenche et al., 2023; Mitchell, 1980).

Zeolite Y has the faujasite framework, a crystalline network of silicon, aluminium, and oxygen atoms. A framework aluminium atom introduces a negative charge balanced by a proton on a neighbouring oxygen, forming a Brønsted acid site. Figure 2.1 shows the supercage and its twelve-membered-ring opening. Removal of framework aluminium removes the associated acid site and can leave silanol groups on neighbouring framework oxygens (Malola et al., 2012).

Figure 2.1: Structure of Zeolite Y showing the supercage and its twelve-membered-ring opening

## 2.2 Dealumination by Steam

Steam hydrolyses framework Al–O–Si bonds during catalyst regeneration. Density functional theory (DFT) calculations by Malola et al. (2012) described dealumination as a sequence of water-assisted bond-cleavage steps. Their calculated effective barriers depended on the reference state for incoming water, demonstrating the role of adsorption thermochemistry in reaction energetics. Figure 2.2 presents their calculated reaction paths for dealumination and desilication.

Figure 2.2: Calculated reaction paths for dealumination and desilication using gas-phase and adsorbed water references

Silaghi et al. (2016) examined dealumination in several zeolite frameworks and discussed how extra-framework aluminium could remain confined within the pores. Their work supported a stepwise description of hydrolysis. Steam hydrolysis therefore provides the baseline reaction for assessing additional effects associated with vanadium.

## 2.3 Vanadium under Regenerator Conditions

Vanadium in a regenerated catalyst is commonly associated with oxidised species, including vanadium pentoxide. Wormsbecher et al. (1986) proposed that vanadium pentoxide reacts with steam to form volatile vanadic acid:

V2O5(s) + 3 H2O(g) ⇌ 2 H3VO4(g)	(2.1)

Equation (2.1) represents the gas-phase vanadic-acid source in the proposed route. Wormsbecher et al. (1986) discussed regenerator conditions near 730 °C, with about 20% steam at a total pressure of 2 atm, and estimated vanadic-acid concentrations in the low-parts-per-million range. Trujillo et al. (1997) considered the same high-steam environment and calculated an H3VO4 partial pressure of about 3.37 × 10-6 atm, corresponding to approximately 1.7 ppm at 2 atm. Appendix B.1 shows the pressure conversion used for the reported gas composition.

Occelli (1991) reviewed interactions of vanadium species with cracking catalysts and described changes in vanadium speciation during steaming and hydrolysis. Trujillo et al. (1997) proposed that vanadium could reach acid sites and form vanadic acid in the presence of water. Their local-enrichment proposal provides a pore-scale context for the acid-site comparison in this study.

## 2.4 Proposed Explanations for Vanadium-Related Damage

Three explanations are central to vanadium-related damage. The vanadic-acid route assigns H3VO4 a direct role in framework hydrolysis. The steam-dominated route assigns the principal attack to water and a catalytic or secondary role to vanadium. The sodium-mediated route proposes that vanadium mobilises sodium, after which sodium hydroxide attacks the framework. Table 2.1 summarises these proposed mechanisms and the studies supporting them.

Table 2.1: Proposed explanations for vanadium-related damage to Zeolite Y

| Proposed mechanism | Proposed role of vanadium | Evidence discussed in the literature |
| --- | --- | --- |
| Vanadic-acid route | H3VO4 directly promotes framework hydrolysis | Vanadium species in steamed catalysts and proposed acid-site chemistry, Wormsbecher et al. (1986) and Trujillo et al. (1997) |
| Steam-dominated route | Steam hydrolyses the framework and vanadium is secondary or catalytic | Similar apparent activation energies for vanadium-loaded and control catalysts, and damage to silicalite, Pine (1990) |
| Sodium-mediated route | Vanadium helps mobilise sodium and steam enables NaOH attack | Dependence of destruction on sodium availability and experiments with sodium vanadate, Xu et al. (2002) |

Pine (1990) reported similar apparent activation energies for destruction of ultra-stable Y zeolite under vanadium-loaded and control conditions. He also reported damage to silicalite, which contains little framework aluminium. These observations support a steam-led contribution and place vanadium's role within the broader catalyst environment.

Xu et al. (2002) proposed that vanadium and sodium act together. In their mechanism, vanadium-containing species mobilise sodium, and steam enables sodium hydroxide formation and framework attack. This pathway makes sodium availability a relevant variable alongside the vanadic-acid and steam routes in Table 2.1.

## 2.5 Evidence of Damage and Mitigation

Etim et al. (2016) examined vanadium-contaminated ultra-stable Y zeolite after steaming and reported changes in the framework and micropore structure. Figure 2.3 presents transmission electron micrographs from their study. These structural observations establish damage under the combined treatment and motivate molecular studies of the elementary steps.

Figure 2.3: Transmission electron micrographs of ultra-stable Y zeolite before and after vanadium contamination and steaming

Wormsbecher et al. (1986) reported catalyst protection by basic oxides under their test conditions. Etim et al. (2018) evaluated a magnesium–yttrium oxide trap and linked vanadium capture to formation of immobile yttrium vanadate. These studies demonstrate the practical importance of vanadium control and connect molecular speciation with catalyst performance.

## 2.6 Computational Studies and Research Context

Periodic DFT studies have calculated water-driven dealumination pathways in zeolites (Malola et al., 2012; Silaghi et al., 2016). Tielens and Dzwigaj (2010) studied acid-base sites in vanadium redox zeolites, focusing on vanadium incorporated within the framework. The present comparison complements these studies by evaluating an external vanadic-acid molecule and water at the same Zeolite Y Brønsted acid site.

Together, these studies describe steam-assisted hydrolysis, vanadium–zeolite interactions, and sodium-mediated damage as relevant parts of RFCC catalyst chemistry. These mechanisms provide context for the adsorption, pathway, and thermochemical comparisons in Chapter Four.

CHAPTER THREE

# 3.0 METHODOLOGY

## 3.1 Computational Workflow and Resources

The calculations modelled vanadic acid and water at one Zeolite Y Brønsted acid site. They evaluated optimised structures, electronic adsorption energies, candidate reaction paths, and harmonic thermochemistry. GFN2-xTB provided the Tier 1 screening calculations, which were run with ORCA 6.1.0 on a Dell Latitude E6430 laptop with 16 GB of memory and one processor core. Tier 2 DFT calculations were run with ORCA 6.1.1 on a cloud virtual machine using four MPI processes (Neese, 2025). Molecular structures were prepared and checked with Spartan and Avogadro; Python scripts processed ORCA outputs and calculation registers. Figure 3.1 summarises the structure-screening, DFT, pathway, and thermochemistry stages.

Figure 3.1: Structure-screening, DFT, pathway, and thermochemistry workflow

## 3.2 Zeolite Y Cluster and Adsorbate Models

The gas-phase cluster had formula AlSi4O4H13 and contained 22 atoms. It represented one framework aluminium atom, four neighbouring silicon atoms, four bridging oxygen atoms, twelve terminal hydrogen atoms, and one proton on a bridging oxygen. The protonated oxygen formed the model Brønsted acid site, and terminal hydrogens capped bonds at the cluster boundary. The cluster, vanadic acid, and water were treated as neutral singlets.

The twelve terminal hydrogen atoms were held fixed during geometry optimisation. Aluminium, silicon, bridging oxygen atoms, and the Brønsted proton were allowed to relax. Vanadic acid was modelled with one V=O bond and three V–OH groups; water was modelled as H2O. Several starting orientations of each adsorbate were prepared near the acid site. Figure 3.2 shows the cluster and isolated reference species.

Figure 3.2: Zeolite Y cluster AlSi4O4H13, vanadic acid, and water used in the calculations

## 3.3 Electronic Structure and Adsorption Energies

The isolated cluster, vanadic acid, and water were optimised with GFN2-xTB. Adsorption complexes were generated by placing each adsorbate in several orientations near the Brønsted proton and optimising each structure. Selected structures and reference species were optimised with B3LYP-D3(BJ)/def2-TZVP using the RIJCOSX approximation, def2/J auxiliary basis, DefGrid3 integration grid, tight self-consistent-field convergence, and tight geometry convergence. Harmonic frequencies were calculated at the same level. PBE0-D3(BJ)/def2-TZVP single-point energies were evaluated on the B3LYP-optimised geometries of the isolated reference species, pre-reaction complexes, and converged post-adsorption minima.

The electronic adsorption energy was calculated using Eq. (3.1):

ΔEads = E(complex) − [E(cluster) + E(adsorbate)]	(3.1)

Equation (3.1) defines the separated cluster and optimised adsorbate as the reference state. A negative ΔEads indicates that the complex has lower electronic energy than the separated species. The relative adsorption-energy difference was calculated using Eq. (3.2):

ΔΔEads = ΔEads(H3VO4) − ΔEads(H2O)	(3.2)

Equation (3.2) assigns negative values to an electronic preference for vanadic acid. Appendix B.2 shows the numerical substitutions for both DFT levels. The adsorption energies reported in Chapter Four are direct electronic values; Appendix A.2 records the counterpoise fragment calculations.

## 3.4 Transition-State Searches

Candidate reaction paths were explored for the vanadic-acid route and a water-hydrolysis control. GFN2-xTB nudged elastic band calculations were followed by eigenvector-following transition-state optimisations (Henkelman & Jónsson, 2000). For each candidate, frequency analysis located the imaginary mode; structures displaced in both directions along that mode were reoptimised to test whether the candidate connected different minima. The pre-reaction complexes are denoted V-PRC (vanadic acid) and W-PRC (water). V-I1 and V-I2 denote successive vanadic-acid pathway states, W-P denotes the water-path post-adsorption minimum, and V-TS2 and W-TS label the transition-state candidates for the two routes.

Acceptance required a converged optimisation, one chemically meaningful imaginary mode, and two displaced structures that relaxed towards different minima. The V-TS2 candidate for the first framework Al–O cleavage step met these Tier 1 criteria. Appendix A.3 records the candidate frequencies, displacement destinations, and final pathway classifications.

## 3.5 Gibbs Energies and Conditional Site Occupation

Harmonic Gibbs energies were obtained from ORCA frequency calculations at 298.15 K and 1003.15 K. The higher temperature represents an RFCC regenerator condition of about 730 °C. The Gibbs energy of adsorption was calculated using Eq. (3.3):

ΔG°ads = G°(complex) − G°(cluster) − G°(adsorbate)	(3.3)

Equation (3.3) evaluates the complex against the separated cluster and isolated molecule at the same temperature. The calculations used ideal-gas, rigid-rotor, harmonic-oscillator thermochemistry at a standard pressure of 1 atm. Appendix B.4 shows the temperature-dependent substitutions for the two pre-reaction complexes.

A conditional competitive-site estimate was calculated at 1003.15 K using the RFCC gas partial pressures reported by Wormsbecher et al. (1986). At 2 atm total pressure, 20% steam gave a water partial pressure of 0.4 atm. At the same pressure, 1–10 ppm vanadic acid corresponded to partial pressures of 2 × 10-6 to 2 × 10-5 atm. Appendix B.1 shows these conversions. The dimensionless standard equilibrium constant for each adsorbate was calculated using Eq. (3.4). Equation (3.5) gives the fraction of sites occupied by each adsorbate:

Ki° = exp[−ΔG°i,ads/(RT)]	(3.4)

θi = Ki°(pi/p°) / [1 + Σj Kj°(pj/p°)]	(3.5)

The leading 1 in Eq. (3.5) represents an unoccupied site. The estimate used one equivalent site, ideal-gas standard states, and independent adsorbates. Equations (3.4) and (3.5) define a conditional model calculation for the stated gas composition. Appendix B.5 provides each numerical substitution and the resulting site fractions.

## 3.6 Data Handling and Acceptance Criteria

ORCA inputs, outputs, final geometries, and calculation registers were retained under `simulation/`. A minimum was classified from geometry convergence and its vibrational frequencies. Frequencies below 20 cm-1 were treated as numerical noise when displacement analysis indicated flat cluster motion; borderline modes were assessed from their displacement behaviour. Transition-state candidates were assessed by optimisation convergence, mode count, and two-sided displacement. Appendix A provides the calculation register for the selected structural and pathway jobs.

CHAPTER FOUR

# 4.0 RESULTS AND DISCUSSION

## 4.1 Local Cluster and Adsorption Structures

GFN2-xTB screening selected starting orientations for vanadic acid and water at the local Zeolite Y acid site. Subsequent B3LYP-D3(BJ)/def2-TZVP optimisations produced the accepted reference, pre-reaction, and post-adsorption minima listed in Table 4.1. The protonated framework Al–O bond in the cluster reference was 1.919 Å, compared with 1.695–1.716 Å for the other three Al–O bonds, identifying the model acid-site distortion.

Table 4.1: Accepted DFT reference and adsorption minima

| State | Optimisation result | Vibrational assessment |
| --- | --- | --- |
| Cluster reference | Converged | One flat reference mode at −4.64 cm-1 |
| H3VO4 | Converged | Minimum, zero imaginary modes |
| H2O | Converged | Minimum, zero imaginary modes |
| V-PRC | Converged | Minimum, zero imaginary modes |
| V-I1 | Converged | Minimum, zero imaginary modes |
| W-PRC | Converged | Minimum, zero imaginary modes |
| W-P | Converged | Minimum, zero imaginary modes |

The cluster's −4.64 cm-1 mode was a flat reference motion; the other accepted DFT minima had zero imaginary modes. Figure 4.1 shows the distinct pre-reaction orientations: vanadic acid approached framework aluminium in V-PRC, whereas water remained farther from aluminium in W-PRC. The selected aluminium–oxygen distances in Table 4.2 quantify these differences and the rearrangements in the post-adsorption structures.

Figure 4.1: Optimised adsorption complexes at B3LYP-D3(BJ)/def2-TZVP. Left, vanadic acid (V-PRC); right, water (W-PRC)

Table 4.2: Selected aluminium–oxygen distances in converged DFT structures (Å)

| Structure | Nearest Al···O distance to adsorbate | Longest framework Al–O distance | Structural interpretation |
| --- | --- | --- | --- |
| Cluster reference | — | 1.919 | Protonated framework reference |
| V-PRC | 1.947 | 2.042 | Vanadic oxygen approached Al and the acid-site Al–O bond lengthened |
| V-I1 | 3.529 | 1.791 | Framework Al–O bonds remained short in the chemisorbed intermediate |
| W-PRC | 3.337 | 1.885 | Water remained outside the Al coordination sphere |
| W-P | 1.718 | 3.129 | Water-derived oxygen approached Al with an elongated framework Al–O bond |

The V-PRC geometry also placed vanadium 2.274 Å from a framework oxygen. In W-PRC, the acid proton lay 1.587 Å from the water oxygen, while a water hydrogen lay 1.825 Å from a framework oxygen; these contacts are consistent with two hydrogen bonds. The direct acid-site association is consistent with the vanadic-acid route proposed by Wormsbecher et al. (1986), and the water contacts accord with the water-assisted interactions studied by Malola et al. (2012); the optimised geometries alone do not establish framework cleavage.

## 4.2 Electronic Adsorption Energies

Table 4.3 shows that both DFT levels favour electronic adsorption of vanadic acid over water. The relative difference, ΔΔEads = ΔEads(H3VO4) − ΔEads(H2O), is negative at each level, as defined in Eq. (3.2). Appendix B.2 gives the numerical substitutions for comparison with the temperature-dependent Gibbs energies in Section 4.4.

Table 4.3: Electronic adsorption energies of vanadic acid and water (kJ mol-1)

| Level of theory | H3VO4 | H2O | ΔΔEads = ΔEads(H3VO4) − ΔEads(H2O) |
| --- | --- | --- | --- |
| GFN2-xTB | −196.9 | −69.6 | −127.3 |
| B3LYP-D3(BJ)/def2-TZVP | −93.01 | −78.32 | −14.69 |
| PBE0-D3(BJ)/def2-TZVP, single point | −93.07 | −78.62 | −14.44 |

B3LYP and PBE0 give similar relative preferences, differing by 0.25 kJ mol-1, so the electronic ranking is consistent across the two hybrid functionals. GFN2-xTB predicts a much larger preference of 127.3 kJ mol-1, about 8.7 times the DFT difference; it therefore provides a screening result rather than a quantitative substitute for the DFT energies. The sign of the DFT preference is consistent with the direct vanadic-acid route proposed by Wormsbecher et al. (1986), although the cited studies do not provide a matched numerical comparison of H3VO4 and H2O at this cluster site, and electronic adsorption energies do not establish a reaction mechanism.

## 4.3 Pathway Energetics

The post-adsorption minima were lower in electronic energy than their respective separated cluster-and-adsorbate references at all three levels of theory (Table 4.4). V-I1 was more stabilised than the water-path minimum W-P at each level, but the size of this difference depended on the method. GFN2-xTB predicted substantially greater stabilisation of V-I1 relative to W-P than either DFT level.

Table 4.4: Relative electronic energies of converged post-adsorption minima (kJ mol-1)

| State | GFN2-xTB | B3LYP-D3(BJ)/def2-TZVP | PBE0-D3(BJ)/def2-TZVP single point |
| --- | --- | --- | --- |
| V-I1 | −385.1 | −115.38 | −120.13 |
| W-P | −65.9 | −24.02 | −22.88 |

The GFN2-xTB search produced a candidate for the first framework Al–O cleavage step in the vanadic-acid route. Table 4.5 reports its energy and imaginary mode alongside the water-path candidate. Appendix A.3 records the two-sided displacement checks, and Appendix B.6 gives the energy substitutions.

Table 4.5: Tier 1 pathway candidates for framework Al–O cleavage and water hydrolysis

| Route and step | Imaginary frequency (cm-1) | Candidate energy above starting minimum (kJ mol-1) | Assessment |
| --- | --- | --- | --- |
| V-I1 to V-I2 | −78.21 | 160.70 | V-TS2 passed the GFN2-xTB Tier 1 and two-sided displacement criteria |
| W-PRC to W-P | −226.10 | 29.29 | W-TS was rejected because both displacements returned to W-PRC |

The V-I1-to-V-I2 candidate lies 160.70 kJ mol-1 above V-I1 and passed the GFN2-xTB displacement criteria, but it is not a validated DFT barrier. The water-path candidate lies 29.29 kJ mol-1 above W-PRC, yet both displacements returned to W-PRC, so its energy is not an accepted activation barrier. The separate DFT V-TS2 optimisation did not converge and had 14 imaginary modes (Appendix A.1); Malola et al. (2012) reported a water-assisted DFT pathway whose effective barrier depended on the water reference state, but no direct barrier comparison is justified here.

## 4.4 Harmonic Gibbs Energies

At 298.15 K, the harmonic adsorption Gibbs energies favoured water over vanadic acid by 11.82 kJ mol-1. At 1003.15 K, the preference increased to 66.36 kJ mol-1, with both pre-reaction complexes having positive standard adsorption Gibbs energies (Table 4.6). The post-adsorption minima also became less favourable as temperature increased: V-I1 shifted from −35.77 to +108.32 kJ mol-1, and W-P shifted from +30.79 to +132.66 kJ mol-1.

Table 4.6: Harmonic standard Gibbs energies of adsorption relative to the separated cluster and adsorbate (kJ mol-1)

| State | ΔG°ads at 298.15 K | ΔG°ads at 1003.15 K |
| --- | --- | --- |
| V-PRC | −17.05 | +133.39 |
| V-I1 | −35.77 | +108.32 |
| W-PRC | −28.87 | +67.03 |
| W-P | +30.79 | +132.66 |

The Gibbs-energy ranking reverses the electronic adsorption preference reported in Section 4.2, and the water advantage widens with temperature because the thermal corrections differ between V-PRC and W-PRC (Appendix B.4). This sensitivity to thermochemical reference states is consistent with Malola et al.'s (2012) finding that the water reference affects calculated dealumination energetics, although their periodic pathway is not directly comparable with this cluster adsorption model. The 1003.15 K values use ideal-gas, rigid-rotor, harmonic-oscillator thermochemistry and do not include pore confinement or coverage-dependent interactions.

## 4.5 Conditional Competitive Site-Occupation Estimate

Using the 1003.15 K Gibbs energies and regenerator partial pressures, the conditional single-site model gives a water fraction of 1.29 × 10-4 and a vanadic-acid fraction of 2.27 × 10-13 to 2.27 × 10-12 (Table 4.7). The resulting water-to-vanadic-acid occupation ratio is 5.7 × 107 to 5.7 × 108; the standard equilibrium constants and substitutions are given in Appendix B.5. At the 3.37 × 10-6 atm H3VO4 partial pressure reported by Trujillo et al. (1997), the calculated ratio is approximately 3.39 × 108.

Table 4.7: Formal single-site occupation estimate at 1003.15 K

| Species or ratio | K° at 1003.15 K | Partial pressure p/p° | Calculated site fraction or ratio |
| --- | --- | --- | --- |
| H3VO4 | 1.13 × 10-7 | 2 × 10-6 to 2 × 10-5 | 2.27 × 10-13 to 2.27 × 10-12 |
| H2O | 3.23 × 10-4 | 0.4 | 1.29 × 10-4 |
| θ(H2O)/θ(H3VO4) | — | — | 5.7 × 107 to 5.7 × 108 |

The model predicts a much greater conditional occupation by water under the stated steam-rich gas composition, in line with the steam-dominated interpretation discussed by Pine (1990). The predicted fractions are small despite their large ratio, so they represent relative competition in the specified equilibrium model rather than measured coverage or reaction rate. The result does not exclude the vanadic-acid route proposed by Wormsbecher et al. (1986): Trujillo et al. (1997) discussed local vanadium enrichment, whereas the present estimate uses bulk gas partial pressures and does not model pore confinement or competing reaction barriers.

---

CHAPTER FIVE

# 5.0 CONCLUSIONS AND RECOMMENDATIONS

## 5.1 Summary of the Study

The study compared vanadic acid and water at a model Zeolite Y Brønsted acid site using a 22-atom AlSi4O4H13 cluster. GFN2-xTB screened structures and pathway candidates, while B3LYP and PBE0 calculations provided the electronic-energy comparison. Harmonic Gibbs energies and a conditional competitive-site estimate were evaluated at regenerator temperature.

## 5.2 Conclusions

1. The optimised AlSi4O4H13 model represented one Zeolite Y Brønsted acid site. Converged vanadic-acid and water structures showed distinct local geometries, as summarised in Tables 4.1 and 4.2.

2. B3LYP-D3(BJ)/def2-TZVP predicted an electronic adsorption preference of 14.69 kJ mol-1 for vanadic acid over water. The PBE0 single-point comparison gave 14.44 kJ mol-1, while GFN2-xTB gave a larger screening-level difference. These values establish a modest, consistent DFT electronic-binding preference for vanadic acid in the cluster model.

3. The GFN2-xTB search yielded a screening-level candidate barrier of 160.70 kJ mol-1 above V-I1 for the first Al–O cleavage step in the vanadic-acid route. Appendix A records the separate DFT frequency and water-path assessments.

4. Harmonic Gibbs energies favoured water over vanadic acid by 11.82 kJ mol-1 at 298.15 K and 66.36 kJ mol-1 at 1003.15 K. Under the stated regenerator partial pressures, the conditional single-site model gave a water-to-vanadic-acid site-fraction ratio of 5.7 × 107 to 5.7 × 108. Appendix B provides the calculation substitutions and model assumptions.

The combined results distinguish electronic binding, temperature-dependent site competition, and pathway energy. They provide a model-level basis for comparing the vanadic-acid route with steam-dominated and sodium-mediated explanations of Zeolite Y dealumination. Pore-aware calculations and catalyst measurements can test the relative contributions of these factors.

## 5.3 Recommendations

1. Extend the adsorption model to a larger cluster or periodic Zeolite Y structure that includes pore confinement, explicit water, and the framework electrostatic environment.

2. Complete a consistent counterpoise correction for both adsorbates and compare the corrected values with the electronic energies reported here.

3. Continue the transition-state search with improved DFT starting geometries, mode verification, and reaction-path calculations for both vanadic-acid and water-hydrolysis routes.

4. Include exchangeable sodium and relevant vanadium species in a follow-up model, then compare the predictions with measurements on steamed, vanadium-contaminated catalysts.

# REFERENCES

Adamo, C., & Barone, V. (1999). Toward reliable density functional methods without adjustable parameters: The PBE0 model. The Journal of Chemical Physics, 110(13), 6158–6170. https://doi.org/10.1063/1.478522

Adanenche, D. E., Aliyu, A., Atta, A. Y., & El-Yakubu, B. J. (2023). Residue fluid catalytic cracking: A review on the mitigation strategies of metal poisoning of RFCC catalyst using metal passivators/traps. Fuel, 343, 127894. https://doi.org/10.1016/j.fuel.2023.127894

Bannwarth, C., Ehlert, S., & Grimme, S. (2019). GFN2-xTB: An accurate and broadly parametrized self-consistent tight-binding quantum chemical method with multipole electrostatics and density-dependent dispersion contributions. Journal of Chemical Theory and Computation, 15(3), 1652–1671. https://doi.org/10.1021/acs.jctc.8b01176

Becke, A. D. (1993). Density-functional thermochemistry. III. The role of exact exchange. The Journal of Chemical Physics, 98(7), 5648–5652. https://doi.org/10.1063/1.464913

Etim, U. J., Xu, B., Ullah, R., & Yan, Z. (2016). Effect of vanadium contamination on the framework and micropore structure of ultra stable Y-zeolite. Journal of Colloid and Interface Science, 463, 188–198. https://doi.org/10.1016/j.jcis.2015.10.049

Etim, U. J., Bai, P., Ullah, R., Subhan, F., & Yan, Z. (2018). Vanadium contamination of FCC catalyst: Understanding the destruction and passivation mechanisms. Applied Catalysis A: General, 555, 108–117. https://doi.org/10.1016/j.apcata.2018.02.011

Grimme, S., Ehrlich, S., & Goerigk, L. (2011). Effect of the damping function in dispersion corrected density functional theory. Journal of Computational Chemistry, 32(7), 1456–1465. https://doi.org/10.1002/jcc.21759

Henkelman, G., & Jónsson, H. (2000). Improved tangent estimate in the nudged elastic band method for finding minimum energy paths and saddle points. The Journal of Chemical Physics, 113(22), 9978–9985.

Lee, C., Yang, W., & Parr, R. G. (1988). Development of the Colle-Salvetti correlation-energy formula into a functional of the electron density. Physical Review B, 37(2), 785–789. https://doi.org/10.1103/PhysRevB.37.785

Malola, S., Svelle, S., Lønstad Bleken, F., & Swang, O. (2012). Detailed reaction paths for zeolite dealumination and desilication from density functional calculations. Angewandte Chemie International Edition, 51(3), 652–655. https://doi.org/10.1002/anie.201104462

Mitchell, B. R. (1980). Metal contamination of cracking catalysts. 1. Synthetic metals deposition on fresh catalysts. Industrial & Engineering Chemistry Product Research and Development, 19(2), 209–213. https://doi.org/10.1021/i360074a015

Neese, F. (2025). Software update: The ORCA program system: Version 6.0. Wiley Interdisciplinary Reviews: Computational Molecular Science, 15, e70019. https://doi.org/10.1002/wcms.70019

Occelli, M. L. (1991). Vanadium-zeolite interactions in fluidized cracking catalysts. Catalysis Reviews: Science and Engineering, 33(3–4), 241–280. https://doi.org/10.1080/01614949108020301

Pine, L. A. (1990). Vanadium-catalyzed destruction of USY zeolites. Journal of Catalysis, 125(2), 514–524. https://doi.org/10.1016/0021-9517(90)90323-C

Silaghi, M.-C., Chizallet, C., Sauer, J., & Raybaud, P. (2016). Dealumination mechanisms of zeolites and extra-framework aluminum confinement. Journal of Catalysis, 339, 242–255. https://doi.org/10.1016/j.jcat.2016.04.021

Tielens, F., & Dzwigaj, S. (2010). Probing acid-base sites in vanadium redox zeolites by DFT calculation and compared with FTIR results. Catalysis Today, 152(1–4), 66–69. https://doi.org/10.1016/j.cattod.2009.09.006

Trujillo, C. A., Navarro Uribe, U., Knops-Gerrits, P.-P., Oviedo A., L. A., & Jacobs, P. A. (1997). The mechanism of zeolite Y destruction by steam in the presence of vanadium. Journal of Catalysis, 168(1), 1–15. https://doi.org/10.1006/jcat.1997.1550

Weigend, F., & Ahlrichs, R. (2005). Balanced basis sets of split valence, triple zeta valence and quadruple zeta valence quality for H to Rn: Design and assessment of accuracy. Physical Chemistry Chemical Physics, 7(18), 3297–3305. https://doi.org/10.1039/b508541a

Wormsbecher, R. F., Peters, A. W., & Maselli, J. M. (1986). Vanadium poisoning of cracking catalysts: Mechanism of poisoning and design of vanadium tolerant catalyst system. Journal of Catalysis, 100(1), 130–137. https://doi.org/10.1016/0021-9517(86)90078-3

Xu, M., Liu, X., & Madon, R. J. (2002). Pathways for Y zeolite destruction: The role of sodium and vanadium. Journal of Catalysis, 207(2), 237–246. https://doi.org/10.1006/jcat.2002.3517

# APPENDICES

## Appendix A. Calculation Register

This register records the accepted DFT minima, incomplete DFT jobs, counterpoise fragment calculations, and transition-state checks used in the thesis. Job identifiers and log files are retained under `simulation/03_tier2_completion/results/` and `simulation/02_tier1/`.

### A.1 DFT structure and pathway jobs

Table A.1 identifies the structures used in Chapter Four and the main incomplete pathway jobs. The register distinguishes converged minima from jobs whose final geometries or frequencies were unavailable.

Table A.1: DFT reference, adsorption, and pathway calculation register

| Method and state | ORCA output | Status and frequency result | Use in thesis |
| --- | --- | --- | --- |
| B3LYP cluster reference | s1_03_cluster_optfreq.out | Converged, one flat reference mode at −4.64 cm-1 | Energy and Gibbs reference |
| B3LYP H3VO4 | s1_02_h3vo4_optfreq.out | Converged minimum, zero imaginary modes | Isolated vanadic-acid reference |
| B3LYP H2O | s1_01_h2o_optfreq.out | Converged minimum, zero imaginary modes | Isolated water reference |
| B3LYP V-PRC | s1_04_vprc_optfreq.out | Converged minimum, zero imaginary modes | Vanadic-acid adsorption energy and geometry |
| B3LYP W-PRC | s1_05_wprc_optfreq.out | Converged minimum, zero imaginary modes | Water adsorption energy and geometry |
| B3LYP V-I1 | s4_01_vi1_optfreq.out | Converged minimum, zero imaginary modes | Post-adsorption minimum |
| B3LYP W-P | s4_04_wp_optfreq.out | Converged minimum, zero imaginary modes | Water-path post-adsorption minimum |
| PBE0 adsorption and post-adsorption single points | pbe0_cluster.out, pbe0_h2o.out, pbe0_h3vo4.out, pbe0_v-prc.out, pbe0_w-prc.out, pbe0_v-i1.out, pbe0_w-p.out | Completed | Electronic-energy comparison in Tables 4.3 and 4.4 |
| B3LYP V-TS2 | s4_05_vts2_optts.out | 200 cycles reached, optimisation unconverged, 14 imaginary modes | DFT transition-state assessment in Appendix A |
| B3LYP V-I2 | first_pass/s4_02_vi2_optfreq.out and s4_02_vi2_optfreq.out | 90- and 60-cycle runs, both unconverged, frequency data unavailable | Excluded from final DFT minima |
| B3LYP V-P | first_pass/s4_03_vp_optfreq.out and s4_03_vp_optfreq.out | 90-cycle run unconverged, 25-cycle run ended before normal completion | Excluded from final DFT minima |

### A.2 Counterpoise fragment calculations

Four manual ghost-fragment jobs were run for the PBE0 counterpoise estimate. Table A.2 records their outcomes. Three jobs completed normally and the V-PRC cluster-fragment job terminated in the LEANSCF step, leaving the fragment set incomplete; the Chapter Four adsorption energies therefore use the direct electronic values.

Table A.2: PBE0 counterpoise ghost-fragment calculation register

| Complex and fragment | Output file | Final status | Final energy / Eh |
| --- | --- | --- | --- |
| V-PRC cluster ghost | v-prc_cp_ghost-cluster.out | LEANSCF error termination | Unavailable |
| V-PRC H3VO4 ghost | v-prc_cp_ghost-h3vo4.out | Normal termination | −1708.714841090478 |
| W-PRC cluster ghost | w-prc_cp_ghost-cluster.out | Normal termination | −76.378622223824 |
| W-PRC H2O ghost | w-prc_cp_ghost-h2o.out | Normal termination | −1708.730926698051 |

### A.3 Tier 1 transition-state and displacement register

Table A.3 summarises the GFN2-xTB candidate structures and the paired mode-displacement results. The vanadic-acid candidate passed the recorded acceptance checks; both water-path displacements returned to W-PRC.

Table A.3: Tier 1 pathway candidate and two-sided displacement register

| Candidate output | Imaginary mode and status | Positive displacement | Negative displacement | Classification |
| --- | --- | --- | --- | --- |
| V-TS2, optts3_bandB_ci.out | −78.21 cm-1 | V-TS2_ts_pos_disp.out → V-I2 well (+15.64 kJ mol-1 vs V-I2) | V-TS2_ts_neg_disp.out → V-I1 well (+107.08 kJ mol-1 vs V-I1) | Accepted GFN2-xTB saddle-point candidate, A1–A5 passed |
| W-TS, optts2_bandD_ci.out | −226.10 cm-1 | W-TS_pos_disp.out → W-PRC well (+1.35 kJ mol-1 vs W-PRC) | W-TS_neg_disp.out → W-PRC well (+1.34 kJ mol-1 vs W-PRC) | Candidate rejected by the two-sided displacement criterion |

## Appendix B. Worked Calculations

Appendix B gives the numerical substitutions behind Tables 4.3–4.7. Energies were converted using 1 Eh = 2625.499638 kJ mol-1. Values are shown to sufficient precision to reproduce the rounded results in Chapter Four.

### B.1 Regenerator partial-pressure conversions

Equation (2.1) describes the proposed formation of gas-phase vanadic acid. At 20% steam and a total pressure of 2 atm, the water partial pressure used in Eq. (3.5) was calculated as shown in Eq. (B.1):

p(H2O) = 0.20 × 2 atm = 0.40 atm	(B.1)

A range of 1–10 ppm H3VO4 at 2 atm gives the partial pressures in Eq. (B.2):

p(H3VO4) = (1–10) × 10-6 × 2 atm = 2 × 10-6 to 2 × 10-5 atm	(B.2)

The 3.37 × 10-6 atm estimate by Trujillo et al. (1997) corresponds to the concentration calculated in Eq. (B.3):

x(H3VO4) = [3.37 × 10-6 atm / 2 atm] × 106 = 1.685 ppm	(B.3)

Equations (B.1)–(B.3) provide the gas composition used in the conditional occupation calculation.

### B.2 Electronic adsorption energies

Using Eq. (3.1), the B3LYP adsorption energy for vanadic acid was calculated from the cluster and isolated-molecule energies. Equation (B.4) gives the reference sum, and Eq. (B.5) subtracts that reference from the V-PRC energy:

E(reference, H3VO4) = −1709.394093884 − 1246.825013959 = −2956.219107843 Eh	(B.4)

ΔEads(H3VO4, B3LYP) = −2956.254531846 − (−2956.219107843) = −0.035424003 Eh	(B.5)

Conversion of Eq. (B.5) to kJ mol-1 is shown in Eq. (B.6):

ΔEads = −0.035424003 × 2625.499638 = −93.0057 kJ mol-1	(B.6)

The water reference sum and W-PRC difference are shown in Eqs. (B.7) and (B.8); Eq. (B.9) gives the converted energy:

E(reference, H2O) = −1709.394093884 − 76.426629796 = −1785.820723680 Eh	(B.7)

ΔEads(H2O, B3LYP) = −1785.850554383 − (−1785.820723680) = −0.029830703 Eh	(B.8)

ΔEads = −0.029830703 × 2625.499638 = −78.3205 kJ mol-1	(B.9)

The B3LYP relative preference from Eq. (3.2) is calculated in Eq. (B.10):

ΔΔEads(B3LYP) = −93.0057 − (−78.3205) = −14.6852 kJ mol-1	(B.10)

The same Eq. (3.1) was applied to the PBE0 single-point values using their own cluster and isolated-molecule references. Equations (B.11)–(B.13) show the vanadic-acid calculation, and Eqs. (B.14)–(B.16) show the water calculation:

E(reference, H3VO4, PBE0) = −1708.736038466 − 1246.479597897 = −2955.215636364 Eh	(B.11)

ΔEads(H3VO4, PBE0) = −2955.251083282 − (−2955.215636364) = −0.035446919 Eh	(B.12)

ΔEads = −0.035446919 × 2625.499638 = −93.0659 kJ mol-1	(B.13)

E(reference, H2O, PBE0) = −1708.736038466 − 76.377725398 = −1785.113763864 Eh	(B.14)

ΔEads(H2O, PBE0) = −1785.143710125 − (−1785.113763864) = −0.029946261 Eh	(B.15)

ΔEads = −0.029946261 × 2625.499638 = −78.6239 kJ mol-1	(B.16)

Equation (B.17) gives the PBE0 preference using Eq. (3.2):

ΔΔEads(PBE0) = −93.0659 − (−78.6239) = −14.4420 kJ mol-1	(B.17)

The substitutions in Eqs. (B.4)–(B.17) produce the DFT entries in Table 4.3. For GFN2-xTB, the separated references are E(reference, H3VO4) = −31.34551236 − 19.77512769 = −51.12064005 Eh and E(reference, H2O) = −31.34551236 − 5.07054445 = −36.41605681 Eh. Applying Eq. (3.1) gives ΔEads(V-PRC) = [−51.19563631 − (−51.12064005)] × 2625.499638 = −196.90 kJ mol-1 and ΔEads(W-PRC) = [−36.44256091 − (−36.41605681)] × 2625.499638 = −69.59 kJ mol-1. Their difference from Eq. (3.2) is −196.90 − (−69.59) = −127.31 kJ mol-1.

### B.3 Relative energies of post-adsorption minima

The post-adsorption energies in Table 4.4 use the separated cluster-and-adsorbate reference for the corresponding route. Equations (B.18) and (B.19) show the Tier 1 values for V-I1 and W-P:

ΔE(V-I1, xTB) = [−51.26731716 − (−51.12064005)] × 2625.499638 = −385.10 kJ mol-1	(B.18)

ΔE(W-P, xTB) = [−36.44113826 − (−36.41605681)] × 2625.499638 = −65.85 kJ mol-1	(B.19)

The corresponding B3LYP calculations appear in Eqs. (B.20) and (B.21), and the PBE0 single-point calculations appear in Eqs. (B.22) and (B.23):

ΔE(V-I1, B3LYP) = [−2956.263052029 − (−2956.219107843)] × 2625.499638 = −115.3754 kJ mol-1	(B.20)

ΔE(W-P, B3LYP) = [−1785.829873928 − (−1785.820723680)] × 2625.499638 = −24.0240 kJ mol-1	(B.21)

ΔE(V-I1, PBE0) = [−2955.261392549 − (−2955.215636364)] × 2625.499638 = −120.1328 kJ mol-1	(B.22)

ΔE(W-P, PBE0) = [−1785.122480008 − (−1785.113763864)] × 2625.499638 = −22.8842 kJ mol-1	(B.23)

### B.4 Harmonic Gibbs-energy substitutions

For each state, the adsorption Gibbs energy was calculated from Eq. (3.3). The harmonic thermal correction is the difference between ΔG°ads and the corresponding electronic ΔEads. Table B.1 lists the B3LYP electronic energies, thermal corrections, and Gibbs energies for the four states in Table 4.6:

Table B.1: Electronic and harmonic Gibbs-energy terms for accepted DFT states (kJ mol-1)

| State | Electronic ΔEads | Thermal correction at 298.15 K | ΔG°ads at 298.15 K | Thermal correction at 1003.15 K | ΔG°ads at 1003.15 K |
| --- | --- | --- | --- | --- | --- |
| V-PRC | −93.0057 | +75.9600 | −17.0457 | +226.4003 | +133.3946 |
| V-I1 | −115.3754 | +79.6007 | −35.7747 | +223.6989 | +108.3235 |
| W-PRC | −78.3205 | +49.4524 | −28.8681 | +145.3513 | +67.0308 |
| W-P | −24.0240 | +54.8185 | +30.7945 | +156.6808 | +132.6568 |

The temperature-dependent values in Table B.1 follow the substitutions in Eqs. (B.24) and (B.25):

ΔG°ads(V-PRC, 298.15 K) = −93.0057 + 75.9600 = −17.0457 kJ mol-1	(B.24)

ΔG°ads(V-PRC, 1003.15 K) = −93.0057 + 226.4003 = +133.3946 kJ mol-1	(B.25)

ΔG°ads(W-PRC, 298.15 K) = −78.3205 + 49.4524 = −28.8681 kJ mol-1	(B.26)

ΔG°ads(W-PRC, 1003.15 K) = −78.3205 + 145.3513 = +67.0308 kJ mol-1	(B.27)

Applying Eq. (3.3) to the two post-adsorption minima gives ΔG°ads(V-I1, 298.15 K) = −115.3754 + 79.6007 = −35.7747 kJ mol-1 and ΔG°ads(V-I1, 1003.15 K) = −115.3754 + 223.6989 = +108.3235 kJ mol-1. For W-P, the corresponding substitutions are ΔG°ads(W-P, 298.15 K) = −24.0240 + 54.8185 = +30.7945 kJ mol-1 and ΔG°ads(W-P, 1003.15 K) = −24.0240 + 156.6808 = +132.6568 kJ mol-1, as listed in Table B.1.

The water-favouring differences at 298.15 K and 1003.15 K are calculated in Eqs. (B.28) and (B.29):

ΔG°ads(V-PRC) − ΔG°ads(W-PRC), 298.15 K = −17.0457 − (−28.8681) = +11.8224 kJ mol-1	(B.28)

ΔG°ads(V-PRC) − ΔG°ads(W-PRC), 1003.15 K = 133.3946 − 67.0308 = +66.3638 kJ mol-1	(B.29)

### B.5 Competitive-site equilibrium constants and fractions

Equation (3.4) was evaluated with R = 0.008314462618 kJ mol-1 K-1 and T = 1003.15 K. The substitutions in Eqs. (B.30) and (B.31) give the standard equilibrium constants:

KH₃VO₄° = exp[−133.3945918 / (0.008314462618 × 1003.15)] = 1.1329138 × 10-7	(B.30)

KH₂O° = exp[−67.0307562 / (0.008314462618 × 1003.15)] = 3.2339647 × 10-4	(B.31)

The pressure-weighted terms qi = Ki°(pi/p°) used in Eq. (3.5) are calculated in Eqs. (B.32)–(B.34):

q(H2O) = 3.2339647 × 10-4 × (0.4/1.0) = 1.2935859 × 10-4	(B.32)

q(H3VO4, 1 ppm) = 1.1329138 × 10-7 × (2 × 10-6/1.0) = 2.2658275 × 10-13	(B.33)

q(H3VO4, 10 ppm) = 1.1329138 × 10-7 × (2 × 10-5/1.0) = 2.2658275 × 10-12	(B.34)

For 1 ppm H3VO4, Eq. (3.5) gives the denominator and fractions in Eqs. (B.35) and (B.36):

D = 1 + 2.2658275 × 10-13 + 1.2935859 × 10-4 = 1.0001293586	(B.35)

θ(H3VO4) = 2.2658275 × 10-13/D = 2.2655344 × 10-13; θ(H2O) = 1.2935859 × 10-4/D = 1.2934186 × 10-4	(B.36)

θ(H2O)/θ(H3VO4), 1 ppm = 1.2934186 × 10-4 / 2.2655344 × 10-13 = 5.7091102 × 108	(B.37)

For 10 ppm H3VO4, the corresponding substitutions appear in Eqs. (B.38) and (B.39):

D = 1 + 2.2658275 × 10-12 + 1.2935859 × 10-4 = 1.0001293586	(B.38)

θ(H3VO4) = 2.2658275 × 10-12/D = 2.2655344 × 10-12; θ(H2O) = 1.2935859 × 10-4/D = 1.2934186 × 10-4	(B.39)

θ(H2O)/θ(H3VO4), 10 ppm = 1.2934186 × 10-4 / 2.2655344 × 10-12 = 5.7091102 × 107	(B.40)

At the H3VO4 partial pressure reported by Trujillo et al. (1997), the pressure-weighted acid term and conditional occupation ratio are:

qH₃VO₄, Trujillo = 1.1329138 × 10-7 × (3.37 × 10-6/1.0) = 3.8179195 × 10-13; θ(H2O)/θ(H3VO4) = 1.2935859 × 10-4 / 3.8179195 × 10-13 = 3.3882 × 108	(B.41)

Equations (B.30)–(B.41) reproduce the range in Table 4.7 and the Trujillo-pressure comparison under the standard-pressure, single-site, ideal-gas harmonic assumptions stated in Section 3.5.

### B.6 Tier 1 candidate barrier substitutions

The GFN2-xTB candidate barrier was calculated from the candidate and starting-minimum energies in the Tier 1 register. Equation (B.42) shows the V-TS2 result; Eq. (B.43) shows the water-path candidate energy difference recorded in Table 4.5.

ΔE‡(V-I1 → V-I2) = [−51.20610884 − (−51.26731716)] × 2625.499638 = 160.7024 kJ mol-1	(B.42)

ΔE‡(W-PRC → W-TS candidate) = [−36.43140308 − (−36.44256091)] × 2625.499638 = 29.2949 kJ mol-1	(B.43)

The W-TS energy difference in Eq. (B.43) is a candidate value; its displacement record and classification are given in Table A.3.